Seagrove Highlands Condominium Owners Association, Inc.

Flooring Modification Requirements

In an effort to reduce the amount of noise which is transmitted from the floors of upper units to the ceilings of those below, the following guidelines must be followed when making modifications to installed floorcoverings. Prior to performing any floor covering changes, an owner must provide a statement that the owner has reviewed the following Requirements and attests that such Requirements will be met by the contracted installation.  In all cases the Grp-Crete gypsum underlayment must not be removed.

- When replacing existing carpet with new carpet the padding used must meet Class 2 specifications such as Bonded Poly-Urethane Foam with a thickness of 3/8” and a density of 6.5 lbs.

- When replacing existing floor covering with any hard surface flooring such as ceramic/porcelain tile, laminate or engineered hardwood that is less than 3/8’, a cork underlayment with a thickness of 1/4” (6mm) shall be used.  The cork backing that may already be attached to the replacement flooring is not to be considered when meeting the 1/4” requirement.  In addition, any adhesive used in attaching the underlayment to the sub-floor and the flooring to the underlayment must be of a type designed for sound absorption, such as Bostik Ultra-Set SingleStep2 or equivalent.

- When replacing existing floor covering with solid stone or hardwood flooring that is 3/8” or greater, an underlayment designed for maximum sound reduction at a thickness of 1/8” (3mm) such as ECO CORK FOAM shall be used.  As set forth above, any adhesive used must be of a type designed for sound absorption and the cork backing that may already be attached to the replacement flooring is not to be considered when meeting the 1/8” requirement.

- When overlaying existing tile flooring with any hard surface flooring such as ceramic/porcelain tile, laminate or engineered hardwood, a cork underlayment with a thickness of 1/8” (3mm) must be used.  The cork backing that may already be attached to the replacement flooring is not to be considered when meeting the 1/8’ requirement.  In addition, any adhesive used in attaching new flooring to the existing floor must be of a type designed for sound absorption, such as Bostik Ultra-Set SingleStep2 or equivalent.

If you have questions or concerns, please contact the Property Manager or a member of the Board of Directors.